## Slide 1
LMST
(in series with 100 ohm resistor)
4.096 V
100 ohm
Adafruit_MCP3421 18 bit ADC
(in parallel with LMST)
Adafruit BNO055 IMU
Adafruit Qwiic / Stemma QT 5 Port Hub
5V
GND
SDA
SCL
Parallel Circuit
Rot Enc
Precision LM4040
Voltage Reference

## Slide 2
r = 0.125”
h = 0.05” (1.27 mm)
Human Knuckle Model
Measured Strain on finger with sample abs_100
(using strings)
~ 0.1677 or 16.8%

## Slide 3
r
h
= 0.25”
Auto Bender Model
Measured Strain on sample abs_100 on AutoBender
~ 0.4 or 40%

## Slide 4
As a reminder….Sample ABS_100
40% elongation

## Slide 5
where
(29.4 x 10^-8 )
, and given the following:
,
where
, so strain normal to x-plane in x direction
,so strain normal to y-plane in y direction
,so strain normal to z-plane in z direction

## Slide 6
References:
Soft Robotics Toolkit. (n.d.). Casting soft robots. Retrieved January 14, 2025,
from https://softroboticstoolkit.com/book/export/html/206021
Craig Jr., R. R. (2011). Mechanics of materials (3rd ed.). Wiley.
Hambley, A.R. (2011). Electrical Engineering Principles and Applications (5th ed.). Prentice Hall.
Callister Jr., W. D., & Rethwisch, D. G. Materials Science and Engineering: An Introduction (10th ed.). Wiley.
Chen, J., Zhang, J., Luo, Z., Zhang, J., Li, L., Su, Y., Gao, X., Li, Y., Tang, W., Cao, C., Liu, Q., Wang, L., & Li, H. (2020).
Superelastic, sensitive, and low hysteresis flexible strain sensor based on wave-patterned liquid metal for
human activity monitoring. ACS Applied Materials & Interfaces, 12(19), 22200–22211.
https://doi.org/10.1021/acsami.0c04709

## Slide 7
Sample Length (not LM channel length)
Previous slide results strained to 40% elongation at L = 1.67”

## Slide 9
44.5% elongation
0.02” x 0.02” square cross-section channels
1.5” sample length
0.25” width
New Sample 11_21_2024
Wire Lead Gauge size CHANGED TO = 30 (from 28)

## Slide 11: Sample 2.27” Long -> will test Monday

## Slide 12: 12_5_2024

## Slide 13: Comparing Sample Lengths
2.31 inches
1.5 inches

## Slide 14: Across Two Samples: 2.3” and 2.31”

## Slide 15: Initial Reapplication Issues
Problem Solved by Adding More Silicone to Inlet

## Slide 16: Reapplication 3x

## Slide 17: Angle Testing: Monday….

## Slide 18: 12/12/2024

## Slide 20: Angle Testing
8 Deg
20 Deg

## Slide 23
Model Data

## Slide 24: 12/19/2024

## Slide 25: Model Curve Changes Drastically When ABS print size changes drastically by 0.001” (0.0254mm)
Changed cross section from 0.02” x 0.02” to 0.014” x 0.014”, so 0.006” height and width

## Slide 26: Model Curve Changes Drastically When ABS print size changes drastically by 0.001” (0.0254mm)
Changed cross section from 0.02” x 0.02” to 0.014” x 0.014”, so 0.006” height and width
0.02” x 0.02”
0.01” x 0.01”

## Slide 27: 4x Reapplication Errorbars: Using MinMax -> 0 to 1 12 prediction files worth of data

## Slide 28: 4x Reapplication Errorbars: Using Norm Res 12 prediction files worth of data

## Slide 29: Misalignment and MinMax: 0, 8, 20 deg 6 prediction files worth of data

## Slide 30: Across Sensor Repeatability: MinMax 12 files, where 1 is trained and is used to predict rest -> 132 prediction files in total

## Slide 32: Rot Enc. Dynamic Test: 100 Cycles, Period is 300 ms, collect 5 data points every 300 ms, 333 deg/sec

## Slide 33: IMU Dynamic Test: 100 Cycles, Period is 300 ms, , collect 5 data points every 300 ms, 333 deg/sec

## Slide 34: IMU Dynamic Test: 100 Cycles, Period is 1 sec, collect 15 data points every 1 sec, 333 deg/sec

## Slide 35: Strain Sensor Dynamic Test: 100 Cycles, Period is 300 ms, collect 5 data points every 300 ms, 333 deg/sec

## Slide 36: Strain Sensor Dynamic Test: 100 Cycles, Period is 1 sec, collect 15 data points every 1 sec, 333 deg/sec

## Slide 37: Comparing peak 0 deg norm res to 100 cycle