## Slide 1
R = 0.125”
h = 0.05” (1.27 mm)
Human Knuckle Model
Measured Strain on finger with sample abs_100
(using strings)
~ 0.1677 or 16.8%

## Slide 2
R
h
= 0.25”
Auto Bender Model
Measured Strain on sample abs_100 on AutoBender
~ 0.4 or 40%

## Slide 3
As a reminder….Sample ABS_100
40% elongation

## Slide 4
Sample Length (not LM channel length)
Previous slide results strained to 40% elongation at L = 1.67”

## Slide 5
44.5% elongation
0.02” x 0.02” square cross-section channels
1.5” sample length
0.25” width
New Sample 11_21_2024
Wire Lead Gauge size CHANGED TO = 30 (from 28)

## Slide 7: Sample 2.27” Long -> will test Monday

## Slide 8: 12_5_2024

## Slide 9: Comparing Sample Lengths
2.31 inches
1.5 inches

## Slide 10: Across Two Samples: 2.3” and 2.31”

## Slide 11: Initial Reapplication Issues
Problem Solved by Adding More Silicone to Inlet

## Slide 12: Reapplication 3x

## Slide 13: Angle Testing: Monday….

## Slide 14: 12/12/2024

## Slide 16: Angle Testing
8 Deg
20 Deg

## Slide 19
Model Data

## Slide 20: 12/19/2024

## Slide 21: Model Curve Changes Drastically When ABS print size changes drastically by 0.001” (0.0254mm)
Changed cross section from 0.02” x 0.02” to 0.014” x 0.014”, so 0.006” height and width

## Slide 22: Model Curve Changes Drastically When ABS print size changes drastically by 0.001” (0.0254mm)
Changed cross section from 0.02” x 0.02” to 0.014” x 0.014”, so 0.006” height and width
0.02” x 0.02”
0.01” x 0.01”

## Slide 23: 4x Reapplication Errorbars: Using MinMax -> 0 to 1 12 prediction files worth of data

## Slide 24: 4x Reapplication Errorbars: Using Norm Res 12 prediction files worth of data

## Slide 25: Misalignment and MinMax: 0, 8, 20 deg 6 prediction files worth of data

## Slide 26: Across Sensor Repeatability: MinMax 12 files, where 1 is trained and is used to predict rest -> 132 prediction files in total

## Slide 27: Rot Enc. Dynamic Test: 100 Cycles, Period is 300 ms, collect 5 data points every 300 ms, 333 deg/sec

## Slide 28: IMU Dynamic Test: 100 Cycles, Period is 300 ms, , collect 5 data points every 300 ms, 333 deg/sec

## Slide 29: IMU Dynamic Test: 100 Cycles, Period is 1 sec, collect 15 data points every 1 sec, 333 deg/sec

## Slide 30: Strain Sensor Dynamic Test: 100 Cycles, Period is 300 ms, collect 5 data points every 300 ms, 333 deg/sec

## Slide 31: Strain Sensor Dynamic Test: 100 Cycles, Period is 1 sec, collect 15 data points every 1 sec, 333 deg/sec

## Slide 32: Comparing peak 0 deg norm res to 100 cycle