## Slide 1
R = 0.125”
h = 0.05” (1.27 mm)
Human Knuckle Model
Measured Strain on finger with sample abs_100
(using strings)
~ 0.1677 or 16.8%

## Slide 2
R
h
= 0.25”
Auto Bender Model
Measured Strain on sample abs_100 on AutoBender
~ 0.4 or 40%

## Slide 3
As a reminder….Sample ABS_100
40% elongation

## Slide 4
Sample Length (not LM channel length)
Previous slide results strained to 40% elongation at L = 1.67”

## Slide 5
44.5% elongation
0.02” x 0.02” square cross-section channels
1.5” sample length
0.25” width
New Sample 11_21_2024
Wire Lead Gauge size CHANGED TO = 30 (from 28)

## Slide 7: Sample 2.27” Long -> will test Monday